PAKISTAN STANDARDS SPECIFICATION

FOR

AMMONIUM SULPHATE, FERTILIZER GRADE

(2ND REVISION)

TABLE-1

Requirements For Ammonium Sulphate, Fertilizer Grade

| S.# | Characteristics | Requirements | Method of Tests Ref Part & Cl. No. |
| --- | --- | --- | --- |
| (1) | (2) | (3) | (4) |
| i) | Moisture, percent by mass, Max | 1.0 | B-3 |
| ii) | Ammonical Nitrogen, percent by mass, Min | 20.6 | B-4 |
| iii) | Free acidity (as H2SO4), percent by mass, Max | 0.025 | B-5 |
| iv) | Arsenic (asAS2O3), ppm, Max | 0.50 | B-6 |

TABLE – III

CRITERION FOR CONFORMITY

| S.# | Characteristic | Test Results 1,2,…… n | Mean | Range | Criterion for Conformity |
| --- | --- | --- | --- | --- | --- |
| i. | ii. | iii | iv | v | vi |
| 1 | Total Ammonical nitrogen, % by weight | -- | X | R | x─0.6 R≥ the value specified in Table (1) |