PS:4883-2018(R)

ICS No.

Pakistan Standard Specification for

Chemical Admixtures for Concrete

(ALL RIGHTS RESERVED)

PAKISTAN STANDARDS AND QUALITY CONTROL AUTHORITY

STANDARDS DEVELOPMENT CENTRE

STANDARDIZATION WING

1ST FLOOR, ST-7-A, BLOCK-3

GULISTAN-E-JOHER

Karachi

TABLE 1 Physical RequirementsA

Type A, Water Reducing

Type B, Retarding

Type C, Acceler- ating

Type D, Water Reducing and Retarding

Type E, Water Reducing and Accelerating

Type F, Water Reducing, High Range

Type G, Water Reducing, High Range

and Retarding

Type S Specific Performance

Water content, max, % of control

95                  ...                      ...                        95                     95                        88                        88                        ...

# Text boxes

| Time of setting, allowable deviation from control, h:min: Initial: at least not more than Final: at least not more than | ... 1:00 earlier nor 1:30 later ... 1:00 earlier | 1:00 later 3:30 later ... 3:30 later | 1:00 earlier 3:30 earlier 1:00 earlier ... | 1:00 later 3:30 later ... 3:30 later | 1:00 earlier 3:30 earlier 1:00 earlier ... | ... 1:00 earlier nor 1:30 later ... 1:00 earlier | 1:00 later 3:30 later ... 3:30 later | 1:00 earlier nor 1:30 later 1:00 earlier |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | nor 1:30 |  |  |  |  | nor 1:30 |  | nor 1:30 |
|  | later |  |  |  |  | later |  | later |
| Compressive strength, min, % of control:B |  |  |  |  |  |  |  |  |
| 1 day | ... | ... | ... | ... | ... | 140 | 125 | ... |
| 3 days | 110 | 90 | 125 | 110 | 125 | 125 | 125 | 90 |
| 7 days | 110 | 90 | 100 | 110 | 110 | 115 | 115 | 90 |
| 28 days | 110 | 90 | 100 | 110 | 110 | 110 | 110 | 90 |
|  | (120)C |  |  | (120)C |  | (120)C | (120)C |  |
| 90 days | (117)C | n/a | n/a | (117)C | n/a | (117)C | (117)C | n/a |
| 6 months | 100 | 90 | 90 | 100 | 100 | 100 | 100 | 90 |
|  | (113)C |  |  | (113)C |  | (113)C | (113)C |  |
| 1 year | 100 | 90 | 90 | 100 | 100 | 100 | 100 | 90 |
| Flexural strength, min, % control:B |  |  |  |  |  |  |  |  |
| 3 days | 100 | 90 | 110 | 100 | 110 | 110 | 110 | 90 |
| 7 days | 100 | 90 | 100 | 100 | 100 | 100 | 100 | 90 |
| 28 days | 100 | 90 | 90 | 100 | 100 | 100 | 100 | 90 |

| requirements):D |  |
| --- | --- |
| Percent of control | 135 | 135 | 135 | 135 | 135 | 135 | 135 | 135 |
| Increase over control | 0.010 | 0.010 | 0.010 | 0.010 | 0.010 | 0.010 | 0.010 | 0.010 |
| Relative durability factor, minE | 80 | 80 | 80 | 80 | 80 | 80 | 80 | 80 |