PS:4533-1999

ICS No.

Pakistan Standard for

Types 1, 2 and 3 Polypropylene (PP) Pipes

General Quality Requirements and Testing

(ALL RIGHTS RESERVED)

PAKISTAN STANDARDS AND QUALITY CONTROL AUTHORITY

STANDARDS DEVELOPMENT CENTRE

(STANDARDIZATION WING),

1ST FLOOR, ST-7-A, BLOCK-3

GULISTAN-E-JAUHAR

Karachi

Table 1

| Test temperature in oC | Exposure medium | PP-H | PP-B | PP-R |  |
| --- | --- | --- | --- | --- | --- |
|  |  | Proof stress, σ0, in N/mm2 | Period of stressing (minimum time to failure), t, in hours | Proof stress, σ0, in N/mm2 | Period of stressing (minimum time to failure), t, in hours | Proof stress, σ0, in N/mm2 | Period of stressing (minimum time to failure), t, in hours |  |
| 20 | Air or water | 21 | 1 | 16 | 1 | 16 | 1 |  |
| 95 | Air or water | 3,5 | 1000 | 2,6 | 1000 | 3,5 | 1000 | Optional |
| 110 | Air | 1,9 | 8760*) | 1,4 | 8760*) | 1,9 | 8760*) | Optional |
| *) For quality control testing performed at the start of production and at any change of material or manufacturing method (valid only temporarily). |  |

Table 3

| Type of pipe | Test temperature, in oC | Minimum period of stressing, t, in mm |
| --- | --- | --- |
| PP-H | 150 ± 2 | 120 ± 2 |
| PP-B | 150 ± 2 | 120 ± 2 |
| PP-R | 135 ± 2 | 120 ± 2 |