PS:4534-1999

ICS No.

Pakistan Standard on

Polypropylene (PP) Pipes Dimensions

(ALL RIGHTS RESERVED)

PAKISTAN STANDARDS AND QUALITY CONTROL AUTHORITY

STANDARDS DEVELOPMENT CENTRE

(STANDARDIZATION WING),

1ST FLOOR, ST-7-A, BLOCK-3

GULISTAN-E-JAUHAR

Karachi

Table 1: Material designation

| Material designation | MRS in N/mm2 |
| --- | --- |
| PP-H 100 1) | 10 |
| PP-B 80 2) | 8 |
| PP-R 80 3) | 8 |
| 1) Previous designation: PP-H (type 1) |
| 2) Previous designation: PP-B (type-2) |
| 3) Previous designation: PP-R (type-3) |

Table 2: Safety factors, SF

| Type of material | Safety factor for a temperature, in oC |
| --- | --- |
|  | From 10 to under 40 | From 40 to 60 | Above 60 |
| PP-H 100 | 1,6 | 1,4 | 1,25 |
| PP-B 80 | 1,25 |
| PP-R 80 |  |

  - Wall thickness and mass

Table 5: Wall thickness tolerances

| Wall thickness, s | Limit deviations1) |  | Wall thickness, s | Limit deviations1) |  | Wall thickness, s | Limit deviations1) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Up to 2 | +0.4 0 |  | Over 22 up to 23 | +2.5 0 |  | Over 43 up to 44 | +4.6 0 |
| Over 2 up to 3 | +0.5 0 |  | Over 23 up to 24 | +2.6 0 |  | Over 44 up to 45 | +4.7 0 |
| Over 3 up to 4 | +0.6 0 |  | Over 24 up to 25 | +2.7 0 |  | Over 45 up to 46 | +4.8 0 |
| Over 4 up to 5 | +0.7 0 |  | Over 25 up to 26 | +2.8 0 |  | Over 46 up to 47 | +4.9 0 |
| Over 5 up to 6 | +0.8 0 |  | Over 26 up to 27 | +2.9 0 |  | Over 47 up to 48 | +5 0 |
| Over 6 up to 7 | +0.9 0 |  | Over 27 up to 28 | +3 0 |  | Over 48 up to 49 | +5.1 0 |
| Over 7 up to 8 | +1 0 |  | Over 28 up to 29 | +3.1 0 |  | Over 49 up to 50 | +5.2 0 |
| Over 8 up to 9 | +1.1 0 |  | Over 29 up to 30 | +3.2 0 |  | Over 50 up to 51 | +5.3 0 |
| Over 9 up to 10 | +1.2 0 |  | Over 30 up to 31 | +3.3 0 |  | Over 51 up to 52 | +5.4 0 |
| Over 10 up to 11 | +1.3 0 |  | Over 31 up to 32 | +3.4 0 |  | Over 52 up to 53 | +5.5 0 |
| Over 11 up to 12 | +1.4 0 |  | Over 32 up to 33 | +3.5 0 |  | Over 53 up to 54 | +5.6 0 |
| Over 12 up to 13 | +1.5 0 |  | Over 33 up to 34 | +3.6 0 |  | Over 54 up to 55 | +5.7 0 |
| Over 13 up to 14 | +1.6 0 |  | Over 34 up to 35 | +3.7 0 |  | Over 55 up to 56 | +5.8 0 |
| Over 14 up to 15 | +1.7 0 |  | Over 35 up to 36 | +3.8 0 |  | Over 56 up to 57 | +5.9 0 |
| Over 15 up to 16 | +1.8 0 |  | Over 36 up to 37 | +3.9 0 |  | Over 57 up to 58 | +6 0 |
| Over 16 up to 17 | +1.9 0 |  | Over 37 up to 38 | +4 0 |  | Over 58 up to 59 | +6.1 0 |
| Over 17 up to 18 | +2 0 |  | Over 38 up to 39 | +4.1 0 |  | Over 59 up to 60 | +6.2 0 |
| Over 18 up to 19 | +2.1 0 |  | Over 39 up to 40 | +4.2 0 |  | Over 60 up to 61 | +6.3 0 |
| Over 19 up to 20 | +2.2 0 |  | Over 40 up to 41 | +4.3 0 |  | Over 61 up to 62 | +6.4 0 |
| Over 20 up to 21 | +2.3 0 |  | Over 41 up to 42 | +4.4 0 |  | Over 62 up to 63 | +6.5 0 |
| Over 21 up to 22 | +2.4 0 |  | Over 42 up to 43 | +4.5 0 |  |  |  |
| 1) The given values have been calculated on the following basis: Limit deviation = 0.1 s + 0.2mm, rounded up to the nearest 0.1mm. A local increase in wall thickness of up to +0.2s is permissible for s up to 10mm, and of up to 0.15 s for s greater than 10mm. The mean of the measurements shall, however, still lie within the given limit deviations. |

Table 6: Allowable working pressure for pipes made from PP-H 100, with SF= 1.25, 1.4, or 1.6

| Temperature in oC | Years of service | Pipe series (S) |
| --- | --- | --- |
|  |  | 20 | 16 | 12.5 | 8.3 | 5 | 3.2 | 2.5 | 2 |
|  |  | Standard dimension ratio (SDR) |
|  |  | 41 | 33 | 26 | 17.6 | 11 | 7.4 | 6 | 5 |
|  |  | Allowable working pressure, in bar |
| 10 | 1 5 10 25 50 100 | 4.5 4.2 4.0 3.8 3.7 3.5 | 5.7 5.2 5.0 4.8 4.6 4.5 | 7.2 6.6 6.4 6.1 5.8 5.6 | 10.9 10.0 9.6 9.2 8.8 8.5 | 18.1 16.6 16.0 15.2 14.6 14.1 | 28.7 26.3 25.3 24.1 23.1 22.3 | 36.1 33.1 31.8 30.4 29.1 28.1 | 45.4 41.7 40.1 38.2 36.6 35.4 |
| 20 | 1 5 10 25 50 100 | 3.9 3.6 3.4 3.3 3.1 3.0 | 4.9 4.5 4.3 4.1 3.9 3.8 | 6.2 5.7 5.5 5.2 5.0 4.8 | 9.4 8.6 8.3 7.8 7.5 7.2 | 15.6 14.2 13.7 13.0 12.5 12.0 | 24.7 22.5 21.7 20.6 19.8 19.0 | 31.1 28.4 27.4 25.9 24.9 23.9 | 39.2 35.7 34.5 32.6 31.3 30.1 |
| 30 | 1 5 10 25 50 100 | 3.4 3.0 2.9 2.8 2.6 2.5 | 4.2 3.8 3.7 3.5 3.3 3.2 | 5.3 4.8 4.6 4.4 4.2 4.0 | 8.0 7.3 7.0 6.6 6.3 6.1 | 13.3 12.1 11.6 11.0 10.5 10.1 | 21.1 19.2 18.4 17.4 16.6 16.0 | 26.6 24.1 23.1 21.9 20.9 20.2 | 33.5 30.4 29.1 27.6 26.3 25.4 |
| 40 | 1 5 10 25 50 100 | 3.3 2.9 2.8 2.6 2.5 2.4 | 4.1 3.7 3.5 3.3 3.2 3.0 | 5.2 4.7 4.4 4.2 4.0 3.8 | 7.8 7.0 6.7 6.3 6.0 5.7 | 13.0 11.7 11.1 10.5 10.0 9.5 | 20.6 18.5 17.6 16.7 15.8 15.1 | 25.9 23.3 22.2 21.0 19.9 19.1 | 32.6 29.4 27.9 26.5 25.1 24.0 |

| Temperature in oC | Years of service | Pipe series (S) |
| --- | --- | --- |
|  |  | 20 | 16 | 12.5 | 8.3 | 5 | 3.2 | 2.5 | 2 |
|  |  | Standard dimension ratio (SDR) |
|  |  | 41 | 33 | 26 | 17.6 | 11 | 7.4 | 6 | 5 |
|  |  | Allowable working pressure, in bar |
| 50 | 1 5 10 25 50 100 | 2.7 2.4 2.3 2.2 2.1 2.0 | 3.4 3.1 2.9 2.7 2.6 2.5 | 4.3 3.9 3.7 3.5 3.3 3.1 | 6.5 5.8 5.6 5.2 5.0 4.7 | 10.8 9.7 9.3 8.7 8.3 7.8 | 17.2 15.4 14.7 13.8 13.1 12.4 | 21.6 19.3 18.5 17.3 16.5 15.6 | 27.2 24.3 23.3 21.8 20.8 19.7 |
| 60 | 1 5 10 25 50 | 2.5 2.2 2.2 2.0 1.9 | 2.3 2.8 2.7 2.5 2.4 | 4.0 3.6 3.4 3.2 3.0 | 6.0 5.4 5.2 4.8 4.5 | 10.1 8.9 8.6 8.0 7.5 | 15.9 14.2 13.7 12.6 11.9 | 20.1 17.8 17.2 15.9 15.0 | 25.3 22.5 21.7 20.0 18.8 |
| 70 | 1 5 10 25 50 | 2.0 1.8 1.7 1.4 1.2 | 2.6 2.3 2.2 1.8 1.5 | 3.2 2.9 2.7 2.2 1.9 | 4.9 4.3 4.1 3.4 2.9 | 8.1 7.2 6.9 5.6 4.8 | 12.9 11.4 10.9 8.9 7.6 | 16.2 14.3 13.7 11.1 9.6 | 20.4 18.0 17.2 14.0 12.0 |
| 80 | 1 5 10 25 | 1.6 1.4 1.2 - | 2.1 1.8 1.5 1.2 | 2.6 2.2 1.8 1.5 | 3.9 3.4 2.8 2.2 | 6.5 5.6 4.6 3.7 | 10.4 8.9 7.3 5.8 | 13.1 11.1 9.2 7.3 | 16.4 14.0 11.6 9.2 |
| 95 | 1 5 (10)1) | 1.2 - - | 1.5 1.0 - | 1.8 1.2 - | 2.8 1.8 (1.5)1) | 4.6 3.0 (2.6)1) | 7.3 4.8 (4.0)1) | 9.2 6.1 (5.1)1) | 11.6 7.6 (6.4)1) |
| The bracketed values apply where testing can be shown to have been carried out for longer than one year at 110oC. |

Table 7: Allowable working pressure for pipes made from PP-H 100, with SF = 1.7

| Temperature in oC | Years of service | Pipe series (S) |
| --- | --- | --- |
|  |  | 20 | 16 | 12.5 | 8.3 | 5 | 3.2 | 2.5 | 2 |
|  |  | Standard dimension ratio (SDR) |
|  |  | 41 | 33 | 26 | 17.6 | 11 | 7.4 | 6 | 5 |
|  |  | Allowable working pressure, in bar |
| 10 | 1 5 10 25 50 100 | 4.3 3.9 3.8 3.6 3.4 3.3 | 5.4 4.9 4.8 4.5 4.3 4.2 | 6.8 6.2 6.0 5.7 5.5 5.3 | 10.2 9.4 9.0 8.6 8.3 8.0 | 17.0 15.6 15.0 14.3 13.7 13.3 | 27.0 24.7 23.8 22.7 21.8 21.0 | 34.0 31.1 30.0 28.6 27.4 26.5 | 42.7 39.2 37.7 36.0 34.5 33.3 |
| 20 | 1 5 10 25 50 100 | 3.7 3.4 3.2 3.1 2.9 2.8 | 4.6 4.2 4.1 3.9 3.7 3.6 | 5.8 5.3 5.1 4.9 4.7 4.5 | 8.8 8.0 7.8 7.3 7.1 6.8 | 14.7 13.4 12.9 12.2 11.7 11.3 | 23.3 21.2 20.5 19.3 18.6 17.9 | 29.3 26.7 25.8 24.4 23.4 22.5 | 36.9 33.6 32.4 30.7 29.5 28.3 |
| 30 | 1 5 10 25 50 100 | 3.2 2.9 2.7 2.6 2.5 2.4 | 4.0 3.6 3.5 3.3 3.1 3.0 | 5.0 4.5 4.3 4.1 3.9 3.8 | 7.6 6.8 6.6 6.2 5.9 5.7 | 12.6 11.4 10.9 10.3 9.9 9.5 | 19.9 18.0 17.3 16.4 15.6 15.1 | 25.1 22.7 21.8 20.6 19.7 19.0 | 31.5 28.6 27.4 25.9 24.8 23.9 |
| 40 | 1 5 10 25 50 100 | 2.7 2.4 2.3 2.2 2.1 2.0 | 3.4 3.0 2.9 2.7 2.6 2.5 | 4.3 3.8 3.6 3.5 3.3 3.1 | 6.4 5.8 5.5 5.2 4.9 4.7 | 10.7 9.6 9.2 8.7 8.2 7.9 | 16.9 15.3 14.5 13.8 13.0 12.5 | 21.3 19.2 18.3 17.3 16.4 15.7 | 26.8 24.2 23.0 21.8 20.6 19.8 |
| 50 | 1 5 10 25 50 100 | 2.2 2.0 1.9 1.8 1.7 1.6 | 2.8 2.5 2.4 2.3 2.2 2.0 | 3.6 3.2 3.0 2.9 2.7 2.6 | 5.4 4.8 4.6 4.3 4.1 3.9 | 8.9 8.0 7.6 7.2 6.8 6.5 | 14.1 12.6 12.1 11.3 10.8 10.2 | 17.8 15.9 15.2 14.3 13.6 12.9 | 22.4 20.0 19.2 18.0 17.1 16.2 |
| 60 | 1 5 10 25 50 | 1.9 1.7 1.6 1.5 1.4 | 2.3 2.1 2.0 1.9 1.7 | 2.9 2.6 2.5 2.3 2.2 | 4.4 4.0 3.8 3.5 3.3 | 7.4 6.6 6.3 5.9 5.5 | 11.7 10.4 10.0 9.3 8.7 | 14.8 13.1 12.6 11.7 11.0 | 18.6 16.5 15.9 14.7 13.9 |
| 70 | 1 5 10 25 50 | 1.5 1.3 1.3 1.0 - | 1.9 1.7 1.6 1.3 1.1 | 2.4 2.1 2.0 1.6 1.4 | 3.6 3.2 3.0 2.5 2.1 | 6.0 5.3 5.0 4.1 3.5 | 9.5 8.4 8.0 6.5 5.6 | 11.9 10.5 10.1 8.2 7.0 | 15.0 13.3 12.7 10.3 8.8 |
| 80 | 1 5 10 25 | 1.2 1.0 - - | 1.5 1.3 1.1 - | 1.9 1.6 1.4 1.1 | 2.9 2.5 2.0 1.6 | 4.8 4.1 3.4 2.7 | 7.6 6.5 5.4 4.3 | 9.6 8.2 6.8 5.4 | 12.1 10.3 8.5 6.5 |
| 95 | 1 5 (10)1) | - - - | 1.1 - - | 1.4 - - | 2.0 1.3 (1.1)1) | 3.4 2.2 (1.9)1) | 5.4 3.5 (3.0)1) | 6.8 4.4 (3.7)1) | 8.5 5.6 (4.7) |
| 1) The bracketed values apply where testing can be shown to have been carried out for longer than one year at 110oC. |

Table 8: Allowable working pressure for pipes made from PP-B 80, with SF = 1.25

| Temperature in oC | Years of service | Pipe series (S) |
| --- | --- | --- |
|  |  | 20 | 16 | 12.5 | 8.3 | 5 | 3.2 | 2.5 | 2 |
|  |  | Standard dimension ratio (SDR) |
|  |  | 41 | 33 | 26 | 17.6 | 11 | 7.4 | 6 | 5 |
|  |  | Allowable working pressure, in bar |
| 10 | 1 5 10 25 50 100 | 4.9 4.6 4.5 4.3 4.2 4.0 | 6.2 5.8 5.6 5.4 5.2 5.1 | 7.8 7.3 7.1 6.8 6.6 6.4 | 11.8 11.1 10.7 10.3 10.0 9.7 | 19.6 18.4 17.7 17.1 16.6 16.1 | 31.1 29.1 28.1 27.1 26.3 25.6 | 39.2 36.6 35.4 34.1 33.1 32.2 | 49.3 46.1 44.5 42.9 41.7 40.5 |
| 20 | 1 5 10 25 50 100 | 4.2 3.9 3.8 3.6 3.5 3.4 | 5.2 4.9 4.7 4.5 4.4 4.2 | 6.6 6.2 6.0 5.7 5.5 5.3 | 10.0 9.3 9.0 8.6 8.4 8.1 | 16.6 15.5 15.0 14.4 13.9 13.4 | 26.3 24.5 23.8 22.8 22.0 21.3 | 33.1 30.9 29.9 28.7 27.7 26.8 | 41.7 38.9 37.7 36.1 34.9 33.7 |
| 30 | 1 5 10 25 50 100 | 3.5 3.2 3.1 3.0 2.9 2.8 | 4.4 4.1 3.9 3.8 3.6 3.5 | 5.6 5.1 5.0 4.8 4.6 4.4 | 8.4 7.8 7.5 7.2 6.9 6.7 | 14.0 12.9 12.5 12.0 11.5 11.2 | 22.3 20.5 19.7 19.0 18.2 17.7 | 28.0 25.8 24.8 23.9 22.9 22.3 | 35.3 32.5 31.3 30.1 38.9 28.1 |
| 40 | 1 5 10 25 50 100 | 2.9 2.7 2.6 2.5 2.3 1.9 | 3.7 3.4 3.3 3.1 2.9 2.4 | 4.6 4.3 4.1 3.9 3.7 3.1 | 7.0 6.4 6.2 6.0 5.6 4.6 | 11.7 10.7 10.4 9.9 9.3 7.7 | 18.5 16.9 16.4 15.7 14.7 12.1 | 23.2 21.3 20.7 19.7 18.5 15.3 | 29.3 26.9 26.1 24.9 23.3 19.2 |
| 50 | 1 5 10 25 50 100 | 2.4 2.2 2.1 1.8 1.5 1.3 | 3.9 2.8 2.7 2.3 1.9 1.6 | 3.8 3.5 3.4 2.9 2.4 2.0 | 5.8 5.3 5.1 4.4 3.6 3.1 | 9.6 8.8 8.5 7.3 6.1 5.1 | 15.2 13.9 13.4 11.6 9.6 8.1 | 19.1 17.5 16.9 14.7 12.1 10.2 | 24.1 22.1 21.2 18.4 15.2 12.8 |
| 60 | 1 5 10 25 50 | 2.0 1.8 1.6 1.2 1.0 | 2.5 2.3 2.0 1.6 1.3 | 3.1 2.9 2.5 2.0 1.7 | 4.7 4.3 3.7 3.0 2.5 | 7.8 7.2 6.2 4.9 4.2 | 12.4 11.4 9.9 7.8 6.6 | 15.6 14.3 12.4 9.9 8.3 | 19.6 18.0 15.6 12.4 10.4 |
| 70 | 1 5 10 25 50 | 1.6 1.3 1.1 - - | 2.0 1.7 1.4 1.1 - | 2.5 2.1 1.7 1.3 1.1 | 3.8 3.2 2.6 2.0 1.7 | 6.4 5.3 4.3 3.4 2.9 | 10.1 8.3 6.8 5.3 4.6 | 12.7 10.5 8.6 6.7 5.7 | 16.0 13.2 10.8 8.4 7.2 |
| 80 | 1 5 10 25 | 1.3 - - - | 1.6 1.2 1.0 - | 2.0 1.5 1.2 1.0 | 3.1 2.2 1.8 1.4 | 5.1 3.7 3.0 2.4 | 8.1 5.8 4.8 3.8 | 10.2 7.3 6.1 4.8 | 12.8 9.2 7.6 6.0 |
| 95 | 1 5 (10)1) | - - - | 1.1 - - | 1.3 - - | 2.0 1.3 (1.2)1) | 3.4 2.2 (1.9)1) | 5.3 3.5 (3.0)1) | 6.7 4.5 (3.8)1) | 8.4 5.6 (4.8)1) |
| 1) The bracketed values apply where testing can be shown to have been carried out for longer than one year at 110oC. |

Table 9: Allowable working pressure for pipes made from PP-B 80 propylene, with SF=1.5

| Temperature in oC | Years of service | Pipe series (S) |
| --- | --- | --- |
|  |  | 20 | 16 | 12.5 | 8.3 | 5 | 3.2 | 2.5 | 2 |
|  |  | Standard dimension ratio (SDR) |
|  |  | 41 | 33 | 26 | 17.6 | 11 | 7.4 | 6 | 5 |
|  |  | Allowable working pressure, in bar |
| 10 | 1 5 10 25 50 100 | 4.1 3.8 3.7 3.6 3.5 3.4 | 5.2 4.8 4.7 4.5 4.4 4.2 | 6.5 6.1 5.9 5.7 5.5 5.3 | 9.8 9.2 8.9 8.6 8.3 8.1 | 16.4 15.3 14.8 14.2 13.8 13.4 | 25.9 24.2 23.4 22.6 21.9 21.3 | 32.6 30.5 29.5 28.4 27.6 26.8 | 41.1 38.4 37.1 35.8 34.7 33.7 |
| 20 | 1 5 10 25 50 100 | 3.5 3.2 3.1 3.0 2.9 2.8 | 4.4 4.1 4.0 3.8 3.7 3.5 | 5.5 5.1 5.0 4.8 4.6 4.4 | 8.3 7.8 7.5 7.2 7.0 6.7 | 13.8 12.9 12.5 12.0 11.6 11.2 | 21.9 20.4 19.8 19.0 18.3 17.7 | 27.6 25.7 24.9 23.9 23.1 22.3 | 34.7 32.4 31.4 30.1 29.1 28.1 |
| 30 | 1 5 10 25 50 100 | 2.9 2.7 2.6 2.5 2.4 2.3 | 3.7 3.4 3.3 3.2 3.0 2.9 | 4.7 4.3 4.1 4.0 3.8 3.7 | 7.0 6.5 6.2 6.0 5.8 5.6 | 11.7 10.8 10.4 10.0 9.6 9.3 | 18.6 17.1 16.4 15.8 15.2 14.8 | 23.4 21.5 20.7 19.9 19.1 18.6 | 29.4 27.1 26.1 25.1 24.1 23.4 |
| 40 | 1 5 10 25 50 100 | 2.4 2.2 2.2 2.1 1.9 1.6 | 3.1 2.8 2.7 2.6 2.4 2.0 | 3.9 3.5 3.4 3.3 3.1 2.5 | 5.8 5.4 5.2 5.0 4.6 3.8 | 9.7 8.9 8.6 8.2 7.7 6.4 | 15.4 14.1 13.7 13.1 12.2 10.1 | 19.4 17.8 17.3 16.5 15.4 12.7 | 24.4 22.4 21.7 20.7 19.4 16.0 |
| 50 | 1 5 10 25 50 100 | 2.0 1.8 1.8 1.5 1.3 1.1 | 2.5 2.3 2.2 1.9 1.6 1.3 | 3.2 2.9 2.8 2.4 2.0 1.7 | 4.8 4.4 4.2 3.7 3.0 2.6 | 8.0 7.3 7.0 6.1 5.1 4.3 | 12.6 11.6 11.2 9.7 8.0 6.7 | 15.9 14.6 14.1 12.2 10.1 8.5 | 20.0 18.4 17.7 15.4 12.7 10.7 |
| 60 | 1 5 10 25 50 | 1.6 1.5 1.3 1.0 - | 2.1 1.9 1.6 1.3 1.1 | 2.6 2.4 2.1 1.6 1.4 | 3.9 3.6 3.1 2.5 2.1 | 6.5 6.0 5.2 4.1 3.5 | 10.3 9.5 8.2 6.5 5.5 | 13.0 11.9 10.4 8.2 6.9 | 16.4 15.0 13.0 10.4 8.7 |
| 70 | 1 5 10 25 50 | 1.3 1.1 - - - | 1.7 1.4 1.1 - - | 2.1 1.7 1.4 1.1 1.0 | 3.2 2.6 2.2 1.7 1.4 | 5.3 4.4 3.6 2.8 2.4 | 8.4 7.0 5.7 4.4 3.8 | 10.6 8.8 7.2 5.6 4.8 | 13.4 11.0 9.0 7.0 6.0 |
| 80 | 1 5 10 25 | 1.1 - - - | 1.3 1.0 - - | 1.7 1.2 1.0 - | 2.6 1.8 1.5 1.2 | 4.3 3.1 2.5 2.0 | 6.7 4.8 4.0 3.2 | 8.5 6.1 5.0 4.0 | 10.7 7.7 6.3 5.0 |
| 95 | 1 5 (10)1) | - - - | - - - | 1.1 - - | 1.7 1.1 (1.0)1) | 2.8 1.9 (1.6)1) | 4.4 3.0 (2.5)1) | 5.6 3.7 (3.2)1) | 7.0 4.7 (4.0)1) |
| 1) The bracketed values apply where testing can be shown to have been carried out for longer than one year at 110oC. |

Table 10: Allowable working pressure for pipes made from PP-R 80, with SF=1.25

| Temperature in oC | Years of service | Pipe series (S) |
| --- | --- | --- |
|  |  | 20 | 16 | 12.5 | 8.3 | 5 | 3.2 | 2.5 | 2 |
|  |  | Standard dimension ratio (SDR) |
|  |  | 41 | 33 | 26 | 17.6 | 11 | 7.4 | 6 | 5 |
|  |  | Allowable working pressure, in bar |
| 10 | 1 5 10 25 50 100 | 5.3 5.0 4.9 4.7 4.6 4.5 | 6.7 6.3 6.1 5.9 5.8 5.6 | 8.4 7.9 7.7 7.4 7.2 7.1 | 12.7 12.0 11.6 11.2 10.9 10.7 | 21.1 20.0 19.3 18.7 18.2 17.7 | 33.4 31.6 30.6 29.6 28.8 28.1 | 42.0 39.8 38.5 37.3 36.3 35.4 | 52.9 50.1 48.5 46.9 45.7 44.5 |
| 20 | 1 5 10 25 50 100 | 4.5 4.2 4.1 4.0 3.9 3.8 | 5.7 5.4 5.2 5.0 4.9 4.7 | 7.2 6.7 6.5 6.4 6.2 6.0 | 10.8 10.2 9.9 9.6 9.3 9.0 | 18.0 16.9 16.4 16.0 15.5 15.0 | 28.6 26.8 26.1 25.3 24.5 23.8 | 36.0 33.8 32.8 31.8 30.9 29.9 | 45.3 42.5 41.3 40.1 38.9 37.7 |
| 30 | 1 5 10 25 50 100 | 3.8 3.6 3.5 3.4 3.3 3.2 | 4.8 4.5 4.4 4.2 4.1 4.0 | 6.1 5.7 5.5 5.3 5.2 5.1 | 9.2 8.6 8.4 8.1 7.9 7.7 | 15.3 14.4 13.9 13.4 13.1 12.8 | 24.3 22.8 22.0 21.3 20.7 20.2 | 30.6 28.7 27.7 26.8 26.1 25.5 | 38.5 36.1 34.9 33.7 32.9 32.1 |
| 40 | 1 5 10 25 50 100 | 3.2 3.0 3.0 2.8 2.8 2.7 | 4.1 3.8 3.7 3.6 3.5 3.4 | 5.1 4.8 4.7 4.5 4.4 4.3 | 7.8 7.3 7.1 6.8 6.6 6.4 | 12.9 12.1 11.8 11.3 11.0 10.7 | 20.5 19.2 18.7 18.0 17.5 16.9 | 25.8 24.2 23.6 22.6 22.0 21.3 | 32.5 30.5 29.7 28.5 27.7 26.9 |
| 50 | 1 5 10 25 50 100 | 2.8 2.6 2.5 2.4 2.3 2.2 | 3.5 3.2 3.1 3.0 2.9 2.8 | 4.4 4.1 3.9 3.8 3.7 3.6 | 6.6 6.1 6.0 5.8 5.6 5.4 | 11.0 10.2 9.9 9.6 9.3 8.9 | 17.5 16.2 15.7 15.2 14.7 14.2 | 22.0 20.4 19.7 19.1 18.5 17.8 | 27.7 25.7 24.9 24.1 23.3 22.5 |
| 60 | 1 5 10 25 50 | 2.3 2.2 2.1 2.0 1.9 | 2.9 2.7 2.6 2.5 2.4 | 3.7 3.4 3.3 3.2 3.1 | 5.6 5.2 5.0 4.8 4.6 | 9.3 8.6 8.3 8.0 7.7 | 14.7 13.7 13.2 12.6 12.1 | 18.5 17.2 16.6 15.9 15.3 | 23.3 21.7 20.8 20.0 19.2 |
| 70 | 1 5 10 25 50 | 2.0 1.8 1.8 1.5 1.3 | 2.5 2.3 2.2 1.9 1.6 | 3.1 2.9 2.8 2.4 2.0 | 4.7 4.3 4.2 3.6 3.1 | 7.8 7.2 7.0 6.1 5.1 | 12.4 11.4 11.1 9.6 8.1 | 15.6 14.3 14.0 12.1 10.2 | 19.6 18.0 17.6 15.2 12.8 |
| 80 | 1 5 10 25 | 1.6 1.4 1.2 1.0 | 2.1 1.8 1.5 1.2 | 2.6 2.3 1.9 1.5 | 3.9 3.5 2.9 2.3 | 6.5 5.7 4.8 3.8 | 10.4 9.1 7.6 6.1 | 13.1 11.5 9.6 7.6 | 16.4 14.4 12.0 9.6 |
| 95 | 1 5 (10)1) | 1.2 - - | 1.5 1.0 - | 1.8 1.2 (1.0)1) | 2.8 1.8 (1.5)1) | 4.6 3.0 (2.6)1) | 7.3 4.8 (4.0)1) | 9.2 6.1 (5.1)1) | 11.6 7.6 (6.4)1) |
| 1) The bracketed values apply where testing can be shown to have been carried out for longer than one year at 110oC. |

Table 11: Allowable working pressure for pipes made from PP-R 80, with SF=1.5

| Temperature in oC | Years of service | Pipe series (S) |
| --- | --- | --- |
|  |  | 20 | 16 | 12.5 | 8.3 | 5 | 3.2 | 2.5 | 2 |
|  |  | Standard dimension ratio (SDR) |
|  |  | 41 | 33 | 26 | 17.6 | 11 | 7.4 | 6 | 5 |
|  |  | Allowable working pressure, in bar |
| 10 | 1 5 10 25 50 100 | 4.4 4.2 4.0 3.9 3.8 3.7 | 5.6 5.3 3.1 4.9 4.8 4.7 | 7.0 6.6 6.4 6.2 6.0 5.9 | 10.6 10.0 9.7 9.4 9.1 8.9 | 17.6 16.6 16.1 15.6 15.2 14.8 | 27.8 26.4 25.5 24.7 24.0 23.4 | 35.0 33.2 32.1 31.1 30.3 29.5 | 44.2 41.8 40.4 39.1 38.1 37.1 |
| 20 | 1 5 10 25 50 100 | 3.8 3.5 3.4 3.3 3.2 3.1 | 4.8 4.5 4.3 4.2 4.1 4.0 | 6.0 5.6 5.5 5.3 5.1 5.0 | 9.0 8.5 8.2 8.0 7.8 7.5 | 15.0 14.1 13.7 13.3 12.9 12.5 | 23.8 22.3 21.7 21.1 20.4 19.8 | 30.0 28.1 27.3 26.5 25.7 24.9 | 37.8 35.4 34.4 33.4 32.4 31.4 |
| 30 | 1 5 10 25 50 100 | 3.2 3.0 2.9 2.8 2.7 2.7 | 4.0 3.8 3.7 3.5 3.4 3.4 | 5.1 4.8 4.6 4.4 4.3 4.2 | 7.7 7.2 7.0 6.7 6.6 6.4 | 12.8 12.0 11.6 11.2 10.9 10.6 | 20.2 19.0 18.3 17.7 17.3 16.9 | 25.5 23.9 23.1 22.3 21.8 21.2 | 32.1 30.1 29.1 28.1 27.4 26.4 |
| 40 | 1 5 10 25 50 100 | 2.7 2.5 2.5 2.4 2.3 2.2 | 3.4 3.2 3.1 3.0 2.9 2.8 | 4.3 4.0 3.9 3.8 3.7 3.5 | 6.5 6.1 5.9 5.7 5.5 5.4 | 10.8 10.1 9.8 9.4 9.2 8.9 | 17.1 16.0 15.6 15.0 14.5 14.1 | 21.5 20.0 19.6 18.8 18.3 17.8 | 27.1 25.4 24.7 23.7 23.1 22.4 |
| 50 | 1 5 10 25 50 100 | 2.3 2.1 2.1 2.0 1.9 1.9 | 2.9 2.7 2.6 2.5 2.4 2.4 | 3.7 3.4 3.3 3.2 3.1 3.0 | 5.5 5.1 5.0 4.8 4.6 4.5 | 9.2 8.5 8.2 8.0 7.7 7.4 | 14.5 13.5 13.1 12.6 12.2 11.8 | 18.3 17.0 16.5 15.9 15.4 14.9 | 23.1 21.4 20.7 20.0 19.4 18.7 |
| 60 | 1 5 10 25 50 | 1.9 1.8 1.7 1.7 1.6 | 2.4 2.3 2.2 2.1 2.0 | 3.1 2.9 2.8 2.6 2.5 | 4.6 4.3 4.2 4.0 3.8 | 7.7 7.2 6.9 6.7 6.4 | 12.2 11.4 11.0 10.5 10.1 | 15.4 14.3 13.8 13.3 12.7 | 19.4 18.0 17.4 16.7 16.0 |
| 70 | 1 5 10 25 50 | 1.6 1.5 1.5 1.3 1.1 | 2.1 1.9 1.9 1.6 1.3 | 2.6 2.4 2.3 2.0 1.7 | 3.9 3.6 3.5 3.0 2.6 | 6.5 6.0 5.9 5.1 4.3 | 10.3 9.5 9.3 8.0 6.7 | 13.0 11.9 11.7 10.1 8.5 | 16.4 15.0 14.7 12.7 10.7 |
| 80 | 1 5 10 25 | 1.4 1.2 1.0 - | 1.7 1.5 1.3 1.0 | 2.2 1.9 1.6 1.3 | 3.3 2.9 2.4 1.9 | 5.5 4.8 4.0 3.2 | 8.6 7.6 6.3 5.1 | 10.9 9.6 8.0 6.4 | 13.7 12.0 10.0 8.0 |
| 95 | 1 5 (10)1) | 1.0 - - | 1.2 - - | 1.5 1.0 - | 2.3 1.5 (1.3)1) | 3.9 2.5 (2.1)1) | 6.1 4.0 (3.4)1) | 7.7 5.0 (4.2)1) | 9.7 6.3 (5.3)1) |
| 1) The bracketed values apply where testing can be shown to have been carried out for longer than one year at 110oC. |

Table 12:	Limit deviations for nominal lengths

| Form (supplied) | Limit deviations |
| --- | --- |
| Coils, unwound length | Actual length not less than nominal length |
| Straight Pipes lengths specified | Up to 12m | ± 10m |
|  | Over 12m | By agreement |